Bayblend� FR 3000

Acrylonitrile Butadiene Styrene + PC

Bayer MaterialScience AG

Product Description

www.fldsj.com

Injection molding grade; easy-flow grade; Vicat/B 120 temperature = 97 �C; UL-listing 94 V-0 (1.5 mm); antimony-, chlorine- and bromine-free flame

retardant; glow wire test (GWFI): 960 �C (2.0 mm); no juicing; good light stability.

General

Material Status

Availability

Features

Forms

Processing Method

• Commercial: Active

• Africa & Middle East

• Antimony Free

• Bromine Free

• Pellets

• Injection Molding

• Europe

• Chlorine Free

• Flame Retardant

• Good Flow

• Good UV Resistance

Physical

Density

Melt volume-flow rate (240�C/5.0 kg)

Molding Shrinkage 3

Across Flow: 240�C, 3.00 mm

Flow: 240�C, 3.00 mm

Water Absorption

Saturation

Equilibrium

Mechanical

Tensile modulus

Tensile Stress

Yield

Break

Tensile Strain

Yield

Break

Impact

Notched Izod Impact Strength

-30�C

23�C

Unnotched Izod Impact Strength (23�C)

Thermal

Deflection Temperature Under Load

0.45 MPa

1.8 MPa

Vicat Softening Temperature

--

50�C/h, B (50N)

CLTE

Flow

Transverse

Page 1 of 2

Nominal Value Unit

1180 kg/m�

24.0 cm�/10min

0.50 to 0.70 %

0.50 to 0.70 %

0.50 %

0.20 %

Nominal Value Unit

2700 MPa

60.0 MPa

45.0 MPa

3.5 %

> 40 %

Nominal Value Unit

10.0 kJ/m�

35.0 kJ/m�

No Break

Nominal Value Unit

92.0 �C

82.0 �C

97.0 �C

95.0 �C

0.000076 cm/cm/�C

0.000080 cm/cm/�C

Test Method

ISO 1183 2

ISO 1133 2

ISO 2577

ISO 62 2

Test Method

ISO 527-2 2

ISO 527-2 2

ISO 527-2/50

ISO 527-2 2

ISO 527-2/50

Test Method

ISO 180/A

ISO 180/1U

Test Method

ISO 75-2 2

ISO 306/B120

ISO 306 2

ISO 11359-2 2

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com

Bayblend� FR 3000

Acrylonitrile Butadiene Styrene + PC

Bayer MaterialScience AG

Electrical

Surface resistivity

Volume resistivity

Relative Permittivity

100 Hz

1 MHz

Dissipation Factor

100 Hz

1 MHz

Comparative tracking index

Electric strength

Flammability

Flame Rating - UL

1.50 mm

2.00 mm

3.00 mm

Notes

1 Typical properties: these are not to be construed as specifications.

2 Tested in accordance with ISO 10350. 23�C/50%r.h. unless otherwise noted.

3 MT: 80�C, 150x105x3 mm

Page 2 of 2

Nominal Value Unit

1.0E+16 ohms

1.0E+14 ohm�m

3.20

3.10

0.0050

0.0060

350

35 kV/mm

Nominal Value Unit

V-0

5VB

5VA

Test Method

IEC 60093 2

IEC 60093 2

IEC 60250 2

IEC 60250 2

IEC 60112 2

IEC 60243-1 2

Test Method

UL 94

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com