CYCOLOY* C1200HF Resin

Acrylonitrile Butadiene Styrene + PC

SABIC Innovative Plastics Asia Pacific

Product Description

www.fldsj.com

PC+ABS, excellent flow/impact/high heat resistance. Low temperature ductility. For automotive, appliance and electrical components.

General

Material Status

Availability

Features

Uses

Forms

Processing Method

• Commercial: Active

• Asia Pacific

• Ductile

• Good Flow

• Appliance Components

• Pellets

• Injection Molding

• Good Impact Resistance

• High Heat Resistance

• Automotive Applications

• Electrical/Electronic

Applications

Physical

Specific Gravity

Melt Mass-Flow Rate (MFR) (260�C/5.0 kg)

Molding Shrinkage - Flow (3.20 mm)

Mechanical

Tensile Modulus 2

Tensile Strength 3(Yield)

Tensile Elongation 3

Yield

Break

Flexural Modulus 4 (50.0 mm Span)

Flexural Strength 4(Yield, 50.0 mm Span)

Impact

Notched Izod Impact

-30�C

23�C

Instrumented Dart Impact

-30�C, Total Energy

23�C, Total Energy

Thermal

Deflection Temperature Under Load

0.45 MPa, Unannealed, 3.20 mm

1.8 MPa, Unannealed, 3.20 mm

Vicat Softening Temperature

CLTE - Flow (-40 to 40�C)

Flammability

Flame Rating - UL (1.19 mm)

UL 746

RTI Str

RTI Imp

RTI Elec

Comparative Tracking Index (CTI) (PLC)

Hot-wire Ignition (HWI) (PLC)

High Amp Arc Ignition (HAI) (PLC)

Injection

Drying Temperature

Drying Time

Drying Time, Maximum

Suggested Max Moisture

Suggested Shot Size

Hopper Temperature

Rear Temperature

Page 1 of 2

Nominal Value Unit

1.15 g/cm�

19 g/10 min

0.50 to 0.70 %

Nominal Value Unit

2280 MPa

57.2 MPa

5.0 %

150 %

2340 MPa

88.3 MPa

Nominal Value Unit

481 J/m

587 J/m

54.2 J

54.2 J

Nominal Value Unit

129 �C

113 �C

130 �C

0.000072 cm/cm/�C

Nominal Value Unit

HB

Nominal Value Unit

105 �C

80.0 �C

105 �C

PLC 2

PLC 3

PLC 1

Nominal Value Unit

100 to 110 �C

3.0 to 4.0 hr

8.0 hr

0.020 %

30 to 80 %

60.0 to 80.0 �C

250 to 290 �C

Test Method

ASTM D792

ASTM D1238

ASTM D955

Test Method

ASTM D638

ASTM D638

ASTM D638

ASTM D790

ASTM D790

Test Method

ASTM D256

ASTM D3763

Test Method

ASTM D648

ISO 306/B50

ASTM E831

Test Method

UL 94

Test Method

UL 746

UL 746

UL 746

UL 746

UL 746

UL 746

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com

CYCOLOY* C1200HF Resin

Acrylonitrile Butadiene Styrene + PC

SABIC Innovative Plastics Asia Pacific

Injection

Middle Temperature

Front Temperature

Nozzle Temperature

Processing (Melt) Temp

Mold Temperature

Back Pressure

Screw Speed

Vent Depth

Notes

1 Typical properties: these are not to be construed as specifications.

2 50 mm/min

3 Type I, 50 mm/min

4 1.3 mm/min

Page 2 of 2

Nominal Value Unit

255 to 295 �C

260 to 300 �C

275 to 300 �C

275 to 300 �C

60.0 to 90.0 �C

0.300 to 0.700 MPa

40 to 70 rpm

0.038 to 0.076 mm

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com