Makrolon� 2865

Polycarbonate

Bayer MaterialScience AG

Product Description

www.fldsj.com

Global grade; MVR (300 �C/1.2 kg) 9.5 cm�/10 min; Chlorine- and bromine-free flame retardant; UL 94V-2/1.5 mm and 3.0 mm; Medium viscosity;

Easy release; Injection molding - Melt temperature 280 - 320 �C; Available in transparent, translucent and opaque colors

General

Material Status

Availability

Features

Appearance

Forms

Processing Method

Multi-Point Data

• Commercial: Active

• Africa & Middle East

• Bromine Free

• Chlorine Free

• Clear/Transparent

• Colors Available

• Pellets

• Injection Molding

• Specific Volume vs

Temperature (ISO 11403-2)

• Europe

• Flame Retardant

• Good Mold Release

• Opaque

• Translucent

• Viscosity vs. Shear Rate (ISO

11403-2)

• Medium Viscosity

Physical

Density

Apparent Density

Melt Mass-Flow Rate (MFR) (300�C/1.2 kg)

Melt volume-flow rate (300�C/1.2 kg)

Molding Shrinkage

Across Flow: 2.00 mm 3

Flow: 2.00 mm 3

Flow

Across Flow

Water Absorption

Saturation

Equilibrium

Mechanical

Tensile modulus

Tensile Stress

Yield

Break

Tensile Strain

Yield

Break

Nominal strain at break

Tensile Creep Modulus

1 hr

1000 hr

Flexural Modulus 4

Flexural Strength 4

3.5% Strain

--

Flexural Strain at Flexural Strength

23�C, 2 mm/min

Page 1 of 4

Nominal Value Unit

1200 kg/m�

0.64 g/cm�

10 g/10 min

9.50 cm�/10min

0.70 %

0.65 %

0.60 to 0.80 %

0.60 to 0.80 %

0.30 %

0.12 %

Nominal Value Unit

2400 MPa

66.0 MPa

70.0 MPa

6.1 %

120 %

> 50 %

2200 MPa

1900 MPa

2400 MPa

73.0 MPa

97.0 MPa

7.1 %

Test Method

ISO 1183 2

ISO 60

ISO 1133

ISO 1133 2

ISO 294-4

ISO 294-4

ISO 2577 2

ISO 2577 2

ISO 62 2

Test Method

ISO 527-2 2

ISO 527-2 2

ISO 527-2/50

ISO 527-2 2

ISO 527-2/50

ISO 527-2 2

ISO 899-1 2

ISO 178

ISO 178

ISO 178

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com

Makrolon� 2865

Polycarbonate

Bayer MaterialScience AG

Films

Carbon Dioxide Permeability

0.0254 mm

0.100 mm

Nitrogen Permeability

0.0254 mm

0.100 mm

Oxygen Permeability

0.0254 mm

0.100 mm

Water Vapor Permeability

23�C, 0.100 mm, 85% RH

Impact

Charpy Notched Impact Strength

-30�C, Complete Break

23�C, Partial Break

Charpy Unnotched Impact Strength

-60�C

-30�C

23�C

Notched Izod Impact Strength

-30�C, Complete Break

23�C, Partial Break

Puncture energy

-30�C

23�C

Puncture - maximum force

-30�C

23�C

Hardness

Ball Indentation Hardness

Thermal

Deflection Temperature Under Load

0.45 MPa

1.8 MPa

Glass Transition Temperature 5

Vicat Softening Temperature

--

50�C/h, B (50N)

Ball Pressure Test (136�C)

CLTE

Flow

Transverse

Thermal Conductivity (23�C)

Page 2 of 4

Nominal Value Unit

16900 cm�/m�/24 hr

4300 cm�/m�/24 hr

510 cm�/m�/24 hr

130 cm�/m�/24 hr

2760 cm�/m�/24 hr

700 cm�/m�/24 hr

15 g/m�/24 hr

Nominal Value Unit

16 kJ/m�

75 kJ/m�

No Break

No Break

No Break

14.0 kJ/m�

85.0 kJ/m�

65.0 J

60.0 J

6300 N

5400 N

Nominal Value Unit

115 MPa

Nominal Value Unit

137 �C

125 �C

150 �C

146 �C

145 �C

Pass

0.000065 cm/cm/�C

0.000065 cm/cm/�C

0.20 W/m/K

Test Method

ISO 2556

ISO 2556

ISO 2556

ISO 15106-1

Test Method

ISO 179/1eA

ISO 179/1eU

ISO 179/1eU 2

ISO 179/1eU 2

ISO 180/A

ISO 6603-2 2

ISO 6603-2 2

Test Method

ISO 2039-1

Test Method

ISO 75-2 2

ISO 11357-2 2

ISO 306/B120

ISO 306 2

IEC 60695-10-2

ISO 11359-2 2

ISO 8302

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com

Makrolon� 2865

Polycarbonate

Bayer MaterialScience AG

Electrical

Surface resistivity

Volume resistivity

Relative Permittivity

100 Hz

1 MHz

Dissipation Factor

100 Hz

1 MHz

Comparative Tracking Index

Solution B

--

Electric strength

Flammability

Flame Rating - UL

0.750 mm

1.50 mm

3.00 mm

6.00 mm

Glow Wire Flammability Index

1.00 mm

1.50 mm

2.00 mm

3.00 mm

4.00 mm

Glow Wire Ignition Temperature

1.00 mm

1.50 mm

2.00 mm

3.00 mm

4.00 mm

Oxygen index

Application of Flame from Small Burner

2.00 mm, Method K and F

Burning Rate (1.00 mm)

Flash Ignition Temperature

Needle Flame Test

1.50 mm, Method F

1.50 mm, Method K

2.00 mm, Method F

2.00 mm, Method K

3.00 mm, Method F

3.00 mm, Method K

Self Ingnition Temperature

UL 746

RTI Str (1.50 mm)

RTI Imp (1.50 mm)

RTI Elec (1.50 mm)

Page 3 of 4

Nominal Value Unit

1.0E+16 ohms

1.0E+14 ohm�m

3.10

3.00

0.00050

0.0090

125 V

225

34 kV/mm

Nominal Value Unit

V-2

V-2

V-2

V-0

850 �C

850 �C

930 �C

960 �C

960 �C

875 �C

875 �C

875 �C

875 �C

875 �C

30 %

K1, F1

Passed

480 �C

60.0 sec

10.0 sec

120.0 sec

20.0 sec

120.0 sec

30.0 sec

550 �C

Nominal Value Unit

125 �C

115 �C

125 �C

Test Method

IEC 60093 2

IEC 60093 2

IEC 60250 2

IEC 60250 2

IEC 60112

IEC 60112 2

IEC 60243-1 2

Test Method

UL 94

IEC 60695-2-12

IEC 60695-2-13

ISO 4589-2 2

DIN 53438-1, -3

ISO 3795

ASTM D1929

IEC 60695-2-2

ASTM D1929

Test Method

UL 746

UL 746

UL 746

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com

Makrolon� 2865

Polycarbonate

Bayer MaterialScience AG

Optical

Refractive Index 6

Transmittance

1000 �m

2000 �m

3000 �m

4000 �m

Haze (3000 �m)

Additional Information

Electrolytical Corrosion

ISO Shortname

Notes

1 Typical properties: these are not to be construed as specifications.

2 Tested in accordance with ISO 10350. 23�C/50%r.h. unless otherwise noted.

3 60x60x2, 500 bar

4 2.0 mm/min

5 10 �C/min

6 Method A

Page 4 of 4

Nominal Value Unit

1.586

89.0 %

89.0 %

88.0 %

87.0 %

< 0.80 %

Nominal Value Unit

A1

PC,MFR,(,,)-09-9

Test Method

ISO 489

ISO 13468-2

ISO 14782

Test Method

IEC 60426

ISO 7391

TEL:0769-88579687  FAX:0769-87792008  Mobile:13751212127  www.fldsj.com